## Slide 1: Extraction chromatography: a novel approch for metal separation
Muhammad Ramzan
Department of Chemistry, UiO
18.03.2015
Hydrometallurgy Seminar, March 2015

## Slide 2: Contents
Introduction
Preparation of Extraction columns
Results
Conclusion
Hydrometallurgy Seminar, March 2015

## Slide 3: Introduction
Extraction chromatography:
Combination:
  Selectivity of liquid-liquid extraction
  Multistage character & rapidity of chromatographic processes
Extractant is adsorbed on the surface of an inert support
Separation of the metals is based on the distribution of the cations of interest between an organic and an aqueous phase
Include the possibility to use mineral acid as mobile phase
Amount of organic compound (ligand) required in extraction chromatography is significantly low
http://www.triskem-international.com/full_extraction_chromatographie.asp
Hydrometallurgy Seminar, March 2015

## Slide 4: Introduction
General parameters of Stationary phases:
Physical stability
  Selection of suitable support
  Eluent parameters
Chemical stability
  Composition of stationary phases change
    Light, temperature & nuclear radiation
  Possible unwanted redox reactions with stationary phases
  TBP strongly hydrolyses in the column, when column left as such after using conc. acids
Regeneration of stationary phases
Repeatability & reproducibility
Hydrometallurgy Seminar, March 2015
Notes: Before u are to going to use extraction chro. For metal separation the following parameters should be kept in mind.
chemically stable, inert and capable of retaining the ligands
pH and electrolyte concentration ( to avoid the loss of extractant from ST. Phases)
It was observed that tetravalent… formed strong complex with extractant
Rt times and area and cycle should be

## Slide 5: Preparation of columns
Extractants dissolved in Methanol:water
(55:45)
Solution is passed through columns
Columns washed with 0.1 M HNO3
Column is ready for separation
Metals can be separated using diluted minerls acid under gradient or isocratic elution
Separated metals detected by ICP-MS or UV/Vis after PCR
Hydrometallurgy Seminar, March 2015
Notes: Very simple recipe to prepare modified column with various ligand density by dissolving appropriate amount of ligand in methanol : water mixture.

## Slide 6: Separation Principle
Hydrometallurgy Seminar, March 2015
RE(III)
RE(III)
RE(III)
RE(III)
RE(III)
Silica bonded with C18
Mobile phase
hydrophilic
Hydrophobic
hydrophilic
Hydrophobic
hydrophilic
Hydrophobic
hydrophilic
Hydrophobic
hydrophilic
Hydrophobic
Notes: The extractant attached with hydrophobic interaction with alkyl chain of c18 and alkyl chin of extractant. The hydrophiclic part that containt functional group id reponcible for complex formation. The metal formed complex and can be eluted with mineal acid used as mobile phase. The elution sequence depend upon the fromation of complex strength.

## Slide 7: Extractants used for impregnation
Hydrometallurgy Seminar, March 2015
H[DEHP]
H[(EH)EHP]
H[TMPeP]

## Slide 8: Separation of REEs
Hydrometallurgy Seminar, March 2015
Intensity (cps)
0
5M
15M
25M
0
10
20
30
40
Time (min)
La
Ce
Pr
Nd
Sm
Eu
Gd
Tb
Dy
Ho
Y
Er
Tm
Yb
Lu
HDEHP
0
2M
6M
10M
14M
0
2
4
6
8
10
12
14
16
18
20
H[TMPeP]
La
Ce
Pr
Nd
Sm
Eu
Gd
Tb
Dy
Ho
Y
Er
Tm
Yb
Lu
0
20M
40M
60M
80M
0
10
20
30
40
H[(EH)EHP]
La
Ce
Pr
Nd
Sm
Eu
Gd
Tb
Dy
Ho
Y
Er
Tm
Yb
Lu
Chromatograms acquired with C18 (250 x 4.6 mm, 5µm, 100Å) modified columns under gradient elution with HNO3 from 0.0 – 2.0 M in 30 min and then 2.0 M isocratic for 20 min at 60oC. The time scale for chromatogram (c) is different from the other two
Notes: Perhaps you should show some chromatograms with all the elements

## Slide 9: Comparsion of Log k
Hydrometallurgy Seminar, March 2015
Chart: Log k
| La | Ce | Pr | Nd | Sm | Eu | Gd | Tb | Dy | Ho | Y | Er | Tm | Yb | Lu
HDEHP | 0.71682 | 0.75582 | 0.77967 | 0.79454 | 0.91728 | 0.97532 | 1.0129 | 1.1218 | 1.1685 | 1.2015 | 1.2389 | 1.2504 | 1.3165 | 1.4002 | 1.4788
Log K (Log D) (obtained in LLEx with (0.75 M HDEHP in toluene and 0.5 M HCl)
Peppard et al., 1957
Log K (retention factor) obtained with
(0.74 mmol HDEHP on C18 column and 0.0-2.0M HNO3 gradient and then 2 M Isocratic)

## Slide 10: Separation of commercial REOs
Hydrometallurgy Seminar, March 2015
0
10M
20M
30M
40M
50M
60M
70M
80M
0
5
10
15
20
25
30
35
Intensity (cps)
Time (min)
La
Ce
Tb
Dy
Ho
Y
Pr
Nd
Sm
Eu
Gd
Chromatograms acquired with C18 (250 x 4.6 mm, 5µm, 100Å) modified columns under gradient elution with HNO3 from 0.0 – 0.5 M in 15 min and then 0.5 – 2.0 M in 15 min at 60oC.
H[(EH)EHP]

## Slide 11
Hydrometallurgy Seminar, March 2015
0.0
0.5M
1.0M
1.5M
2.0M
2.5M
3.0M
0
5
10
15
20
25
30
Time (min)
Tb
Dy
Ho
Y
Er
Tm
Yb
Lu
0.0
0.2M
0.4M
0.6M
0.8M
1.0M
1.2M
1.4M
2
4
6
8
10
12
14
Intensity (cps)
Tb
Dy
Ho
Y
Er
Tm
Yb
Lu
LREEs
LREEs
Separation of commercial REOs
H[TMPeP]
H[(EH)EHP]
Chromatograms acquired with C18 (250 x 4.6 mm, 5µm, 100Å) modified columns under gradient elution with HNO3 from 0.0 – 0.5 M in 15 min and then 0.5 – 2.0 M in 15 min at 60oC for H[(EH)EHP. The gradient condition for H[TMPeP] 0.0 – 0.3 M in 20 min. The time scale for chromatogram obtained with H[TMPeP] is different.
Notes: REOs that contain mainly HREEO are separated on two columns. The EHEHPA column is give excellecnt separation between all REEs but took longer time to elutes but on the other hand HTEHP took shorter time.

## Slide 12: Determination of actinides
Various analytical methods are used to detect very low concentration of actinides
  Neutron activation, alpha spectrometry, thermal ionization mass spectrometry and fission track analysis
ICP-MS is useful for actinide determination.
Methods requires that actinide analytes be separated prior to analysis to resolve analytes with similar mass.
Analysis of plutonium (239Pu) in presence of Uranium (238UH).
Chemical separation methods are time consuming processes
Hydrometallurgy Seminar, March 2015
Dominic S. Peterson et al., Journal of Chromatographic Science, Vol. 47, August 2009
Notes: Require large amount of sample and pre-treatment of sample. Time consuming process.

## Slide 13: Separation of actinides
Hydrometallurgy Seminar, March 2015
Separation of actinide analytes on 100-cm long column, 750 μm i.d. packed with TRU resin. The sample contained 50 ppt of each actinide except thorium, which contained 300 ppt; 400 μL injected. Using gradient elution with oxalic acid.
Octyl(phenyl)-N,N-diisobutylcarbamoylmethylphosphine oxide

## Slide 14: Advantages of impregnated columns
Hydrometallurgy Seminar, March 2015
Commercial columns can be used to design a stationary phase of suitable selectivity for a particular group of elements
Impregnation process is easily performed & amount of extractant loading can be varied to optimize the separation efficiency
Columns may also be re-impregnated with different extractant by easily removing the previously impregnated extractant
Mobile phase could be kept simple (diluted mineral acid)
Impregnation seems to improve the stability of the column towards mineral acid used as eluent
To select suitable extractants, the long-time experience and knowledge from liquid-liquid extraction (LLEx) can be utilized

## Slide 15
Extraction chromatography provides a simple and effective method for the analytical and preparative-scale separation of a variety of metal ions
Advances in support design,most notably the introduction of functionalized supports to enhance metal ion retention, promise to yield further improvements
Impregnation of reversed-phase columns provides large flexibility to design columns for separation of a certain metals
Loading amount of extractant on the stationary phase can be increased or decreased for particular group of elements separation
Conclusions
Hydrometallurgy Seminar, March 2015

## Slide 16
Thanks for listening
Hydrometallurgy Seminar, March 2015